PCB Name:	<Description>	Date: ___________
PCB Item No:	<Item No>	Technology: ☐ Rigid	/ ☐ Rigid-Flex / ☐ Flex

PCB Revision:	<Revision>	Size of PCB:	XX x YY mm

PCB Spec Revision: <Revision>(this doc)	No of layers:	____

Issued by: ___________________________	Thickness:  	____ mm

Specified Stack-up:  ☐  Yes      ☐ No

According to specification in document ___________________

PCB requirements:

IPC 6012 (latest revision), Class 2

UL 94V-0

Electrically Tested

RoHS:		Impedance:

☐Yes		☐ Yes  Acc. to info in stack-up specification

☐ No		☐ No

Material:

☐ FR4 according to IPC 4101/ _______

☐ Other: ________________________

Copper foil thicknesses

Inner layers	Outer layers
(finished copper acc. to IPC-6012, table 3-7)	(finished copper acc. to IPC-6012, table 3-8)

Weight	Weight

☐ 0.5oz	(18µm)	☐ 0.5oz	(18µm) + plating

☐ 1oz	(35µm)	☐ 1oz	(35µm) + plating

☐ 2oz	(70µm)	☐ 2oz	(70µm) + plating

☐              _ 		☐              _

Solder coating / Surface finishes	Electro plated gold

☐ LF-HASL (Lead free)	☐	Electroplated Au (over Ni) according to ASTM B-488,

☐ HASL		purity type 1 (99.7%), hardness code C (130-200 HVN).

☐ OSP	Min thickness according to IPC-6012 table 3-2

☐ ENIG (IPC-4552) 	(Ni min 2.5 μm, Au min 0.8 μm).

☐              _	☐              _

Solder Mask according to IPC SM-840D	Silk screen / Legend print:

☐ No	☐ White

☐ Bottom	☐ Top	☐ Bottom	☐ Top

☐ Green		☐ White

☐ ______________	☐ _____________

Via hole plugging:

☐ Soldermask plugging

☐ Acc. to IPC-4761 type VI (resin)

☐ Acc. to IPC-4761 type VII (resin & capped)

Temporary soldermask:

☐ Peelable mask

☐ Kapton

Technology (via structure):

☐ Blind/buried via holes

☐ Micro vias

☐ Back drilling

Marking:

☐ Date code YYWW

☐ UL

☐ RoHS

☐ Manufacturer Logo

☐_________________

Design parameters:

☐ Min trace width:            ______mm

☐ Min isolation distance: ______mm

☐ Min hole size:                 ______mm

Fabrication enhancement:

Remove non-functional pads                    ☐ Yes     ☐ No

Allowed to add supplementary pattern  ☐ Yes     ☐ No

Other information: